Predicting Phonon Properties using Ab Initio Anharmonic Lattice Dynamics

---
From Ankit…
=
L

---
Phonons
Lattice vibrations (Phonons) are travelling waves:
Waves that can exist depend on system size.
When system is very large (bulk)…
Useful for:
Crystalline materials
Disordered materials
Interfaces
Vibrational Frequencies in Si > Ge
Si Ge
kspring
matom
=
kspring
matom

---
Phonons
Phonons are lattice vibrations:
Waves that can exist depend on system size.
When system is very large (bulk)…
Actual atomic interactions are non-linear.
Interactions in a solid are mostly harmonic with anharmonic perturbation.
kspring
matom

---
Force Constants
Harmonic force constants: under harmonic approximation phonons don’t interact so lifetimes and thermal conductivity are infinite (in a perfect infinite size crystal).
=

---
Phonon Lifetimes
Phonon Interactions:
=3-phonon+4-phonon+…
Waves that can exist depend on system size.
When system is very large (bulk)…
Increasing Temperature
3-phonon
4-phonon
kspring
matom

---
Force Constants
Molecular Dynamics:
Lattice Dynamics:
Harmonic (HLD): Phonons, frequencies, group velocities
Anharmonic (ALD): Phonon lifetimes

---
Calculating Force Constants
Phonon lifetimes
- Forces must be calculated for small displacements.
number of calculations =

---
Calculating Force Constants
Phonon lifetimes
- By recognizing crystal symmetries, there is a huge savings in computational cost.
number of calculations <

---
Ab Initio (Quantum) ALD vs. MD
- ALD force constants = Forces must be calculated for small displacements. Number of force constants number of “timesteps”
- MD time step = Forces must be calculated for small(ish) displacements every timestep.
For Quantum (DFT):
-Si, 500 atom structure	1 minute
MD cost =	(NUMBER_STEPS) X (COST PER STEP)
( 10*longest_lifetime(ps) ) / (timestep (ps) ) X (computer cost per step)
        =	( 10*100 ps) / (0.005 ps) X ( 1 min / step) = 33300 hours
Cost of ALD 1st NN	cost = 4.5 hours
      2nd NN	cost = 367 hours

---
Cost of ALD vs. MD using DFT
-These are computational costs for ALD without applying crystal symmetries.
Si longest_lifetime ~ 100 ps
MD cost =	(NUMBER_STEPS) X (COST PER STEP)
( 10*longest_lifetime(ps) ) / (timestep (ps) ) X (computer cost per step)
        =	( 10*100 ps) / (0.005 ps) X ( 1 min / step) = 33300 hours
ALD number of calculations =
ALD expensive for systems w/ long-range interactions, but usually cheaper than MD.
MD does not include quantum statistical effects

---
ALD Predicts Phonon Properties
Simulation: Classical vs. Quantum
Simulation Expense
Fitted function(al)s using Ab-Initio, expriment, intuition, etc
No fitting, different “environments” naturally accounted for
DFT
3 steps/min/128cpu = 0.023 steps/min/cpu
Stillinger-Weber
6E4 steps/min/4 cpu = 15000 steps/min/cpu
=
J. Appl. Phys. 108, 113524 2010

---
Ankit’s Work using ALD Phonon Properties
Simulation: Classical vs. Quantum
=
Simulation Expense
Fitted function(al)s using Ab-Initio, expriment, intuition, etc
No fitting, different “environments” naturally accounted for
DFT
3 steps/min/128cpu = 0.023 steps/min/cpu
Stillinger-Weber
6E4 steps/min/4 cpu = 15000 steps/min/cpu
L

---
ALD Includes Quantum Effects
Simulation: Classical vs. Quantum
Si Experiment
Simulation Expense
Fitted function(al)s using Ab-Initio, expriment, intuition, etc
No fitting, different “environments” naturally accounted for
DFT
3 steps/min/128cpu = 0.023 steps/min/cpu
Glassbrenner, C. J. and G. A. Slack, Phys. Rev. 134, 4A (1964) A1058-A1069.
Bose-Einstein Statistics (Quantum):
Si Simulation
Stillinger-Weber
6E4 steps/min/4 cpu = 15000 steps/min/cpu
Maxwell Statistics (Classical):
PHYSICAL REVIEW B 79, 224305 2009

---
Phonons are Bosons
There are other things that are Bosons as well:
Photons
Composite particles (He4) (superfluid):
http://demonstrations.wolfram.com/BoseEinsteinFermiDiracAndMaxwellBoltzmannStatistics/

---
Force Constants Constraints

---
Bulk Modulus involves strain of total cell.
This strain energy can be related to the acoustic group velocity.
For short wavelength, there is a lot of strain energy/length. Lots of atoms are displaced from equilibirum. One reason why phonon energy is hbar omega
What kind of phonon mode involve the whole cell getting bigger? Gamma point phonons.

---
From Ankit…